|  | 3rd International Conference Advanced Composite Materials Engineering  COMAT 2010 27- 29 October 2010, Brasov, Romania |
| --- | --- |

COMPOSITE SCREEN WICKS FOR HEAT PIPES

Virgil B. Ungureanu1

1 Transilvania University, Brasov, ROMANIA,  virbung@unitbv.ro

Abstract:  Generally, an optimal wick structure requires high heat conductivity across the wick thickness for a small temperature drop, small surface pores for large capillary pressure, but large internal pores for minimal liquid flow resistance. Screen wicks are most available, because the possibility of their arrangement in different manner on the heat pipe internal wall. The below discussed properties of the wick are represented by the permeability, and the heat conductivity. But the saturated screen wick is a non homogeneous and anisotropic material. The heat conductivity along and across of a screen wick was calculated using series, parallel and mixed model. The experimental measurement carried out for the transversal and longitudinal conductive heat transfer coefficient was served to choice the best model.

Keywords:  heat pipe, wick, composite wick, screen wick, heat conductivity.

1. INTRODUCTION

In the heat pipes operating in gravity body forces and having liquid metals that working fluids wick is absolutely necessary. The experimental results show a high operating instability with great steps in the temperature profile in the absence of the wick. Also, wick is necessary in heat pipes used for the isotherm processes [1], [2].

For a multi layer screen wick from a cylindrical heat pipe was obtained relations that approximate the permeability [1], [3] and [5].

Beginning from a careful observation of the screen wrapping, the new geometric model for the screen wick will be used in order to obtain new relations for the permeability and the equivalent heat conductivity coefficient of a multilayer screen wick.

2. THE PERMEABILITY OF THE WICK

Darcy established in 1856 the equation [5]:

Q=kAefJ,	(1)

In which Q is the volume flow rate, Aef – effective flowing surface area, J - hydraulic pipe pitch and k - the filtration coefficient through the porous medium. But this coefficient k is not a property of the wick, its dimensional formula being length to time ratio. Thus was proposed a new coefficient named permeability that is only a property of the wick structure:

K=kρgη [m2],	(2)

in which ρ is the fluid density, g- the gravity acceleration and η - the dynamic viscosity.

The equation (1) can be written in a manner of Hagen-Poiseuille equation:

Q=k⋅Aef64ηvdhρ⋅ldh⋅v22g⋅1l,	(3)

where dh is the hydraulic diameter, v - velocity and l - length of the liquid flow path. By replacing the volume flow rate:

Q=vA,	(4)

where A is the cross section surface area of the wick it results the permeability:

K=kηρg=AefA⋅dh232.	(5)

It can be demonstrated that the volume porosity is the same as the surface porosity. Thus, the porosity of the wick is defined as:

ε=V0V=AefA,	(6)

in which V0 is the gap volume and V - the overall volume.

Finally it results a relation between the permeability and the porosity:

K=εdh232.	(7)

2. THE SCREEN WICK PERMEABILITY

It is considered a screen wick realized by n screen layer wrapped in a heat pipe having the inner diameterD.

Thus it can be obtained the circumferential length of each screen wick layer, from i=1 to n:

L1=πD−4⋅d1+B0+B;	(8)

L2=πD−4⋅2d1+B0+B;	(9)

…………………………………

Li=πD−4⋅id1+B0+B;	(10)

…………………………………

Ln=πD−4⋅nd1+B0+B.	(11)

The equivalent hydraulic diameter can be defined with relation:

dh=4⋅Flow surface areaWetted perimeter=4⋅Gap volumeWetted surface area,	(12)

where:

Gap volume=π4D2−D−4nd1+B0+B2⋅l⋅ε	(13)

and the wetted surface area is the lateral surface area of longitudinal wires plus the lateral surface area of transversal wires plus the internal area of the heat pipe container. It results the equivalent hydraulic diameter:

dh=4⋅π4⋅D2−D−4nd1+B0+B2⋅l⋅ε2π2dNli=1nD−4d1+B0+bi+πDl	(14)

By replacing the sum of the natural numbers it results:

dh=8ndε1+B0+BD−2nd1+B0+BD+2πdNnDS−4πd2NSnn+11+B0+B.	(15)

and finally:

dh=εd21−ε⋅X1−1X2−X3−1	(16)

in which the symbols represents:

X1=12d1+B0+BnD;	(17)

X2=X1⋅dD81−εn+12;	(18)

X3=X1⋅πd2nNSD41−εn+1.	(19)

By replacing eq. (15) in eq. (7) it results the permeability for a screen wick composed by many wrapped layers:

K=ε3d21281−ε2⋅X1−12D2X2−X3−12.	(20)

3. THE EQUIVALENT HEAT CONDUCTIVITY COEFFICIENTS

The conductive heat transfer along or across of a screen wick was calculated using some series, parallel and mixed analytical models. The experimental measurement carried out for the transversal and longitudinal conductive heat transfer coefficient was served to choice the best models that will be presented.

3.1. The thermal conductivity coefficient across a screen wick

The equivalent thermal conductivity coefficient across a multilayer screen wick considers the diagonal sinuous direction of wires and not only a common heat transfer along the heat flux direction. So, the heat can be partially transferred along the wick.

First it is described a model without the waving coefficient. The filling and warp wires are considered series coupled with the afferent liquid on the screen thickness (2d), the thermal resistance being noted with R1(T) in figure 1. It results:

λ1(T)=λsλlλs−πdN2λs−λl,	(21)

in which λs and λl are the thermal conductivity coefficient of the solid and respectively liquid.

The thermal resistance of the clearance c is considered being series coupled with the above thermal resistance, but it will be composed by two thermal resistances parallel coupled: one composed from the liquid and the other composed by the part due of filling and warp wires waving, in Figure 1 the thermal resistance being R2(T):

λ2(T)=λs2πd24⋅1NS−11N2c+λl⋅1−2πd24⋅S−1N1N2c.	(22)

By introducing the geometric parameters of the screen, it results:

λ2(T)=λl+πdNS−14B0λs−λl.	(23)

Figure 1: The thermal conductivity model across the heat pipe screen wick

By series coupling the above thermal resistances it results the thermal conductivity coefficient of the wick composed by a single screen layer, the equivalent thermal resistance being R0(T)

λw,1(T)=λ1(T)λ2(T)λ1(T)⋅c2d+c+λ2(T)⋅2d2d+c.	(24)

By introducing the geometric parameters of the screen, it results finally:

λw,1(T)=λsλl⋅1+B0⋅λl+πdNS−14B0λs−λlλsλlB0+λl+πdNS−14B0λs−λl⋅λs−πdN2λs−λl.	(25)

For many layers of screen, the thermal conductivity across the wick includes the liquid with the thickness 2Bd, afferent to each layer of screen and will be expressed by the equation:

λw(T)=λw,1⋅λl⋅1+B0+Bλw,1⋅B+λl⋅1+B0.	(26)

3.2. The thermal conductivity coefficient along a screen wick

The model for the thermal conductivity coefficient along the screen wick considers the thermal conduction through the warp wires is partial across the screen because the waving. The analogue electrical scheme is presented in Figure 2.

For the equivalent thermal conductivity of the filling wires series coupled with the afferent liquid, but not considering the waving – in Figure 2 being R1(L) - can be obtained from the equation:

λ1(L)=λsλlλs−πd24Sf⋅1N1N2d+c2⋅λs−λl.	(27)

By introducing the geometric parameters of the screen, it results the equivalent thermal conductivity coefficient of the filling wires series coupled with the afferent liquid:

λ1(L)=λsλlλs−0,25πdSfN⋅λs−λl1+B0.	(28)

Figure 2: The thermal conductivity model along the heat pipe screen wick

The equivalent thermal conductivity coefficient of the waving zone of filling and warp wires (considered with a same waving coefficient Sw), parallel coupled with the liquid from the clearance zone – the thermal resistance being R2(L) in Figure 2) is:

λ2(L)=λl+πd24Sw1N1N2d+c2λs−λl.	(29)

By introducing the geometric parameters of the screen, it results:

λ2(L)=λl+0.25⋅πdSwNλs−λl1+B0.	(30)

Finally, considering the liquid between layers having the thickness 2Bd, it results the equivalent thermal conductivity coefficient along the screen wick:

λw(L)=λ1(L)+λ2(L)1+B0+λlB1+B0+B.	(31)

4. EXPERIMENTAL RESEARCHES

In order to verify the above obtained models it is realized a special box with various number of screen layers and so, different compaction coefficients. The working liquid was the distilled water. The equivalent heat conductivity coefficient of these composite materials was measured with an installation using the plate method. The screen layers are ranged along or across the heat flux of the installation.

Figure 3 shows the results of calculus versus experiences, the line representing the analytical results and dots – the experimental results. For the heat conductivity along the screen wick it is remarked a very good agreement.

| Figure 3: The heat conductivity across and along the heat pipe screen wick |  |
| --- | --- |

5. CONCLUSION

The composite wick is composed by two structures: one for transport and the other for capillary pumping. Thus, the permeability is calculated for the transport structure. Generally, the wick is an anisotropic material. However, the screen wick it an orthotropic material and it can obtain the equivalent thermal conductivity across and along of this kind of wick. Some analytical models are obtained but it is presented the optimal. A good agreement is obtained between the theory and the experimental results.

REFERENCES

- Reay D., Kew P. Heat Pipes. Theory and Applications. Elsevier Science and Technology, 2006.

- Ungureanu, V.B. Structuri capilare compozite pentru tuburile termice gravitaţionale. Conferinta Nationala de Termotehnica, Sibiu, vol.2., 2000.

- Imura H., Kozai H., Ikeda F. The effective Pore Radius of Screen Wicks. Proc. of the 8th International Heat Pipe Conference, Bejing, 1992.

- Kozai H. Transfer Characteristics in Composite Screen Wick Heat Pipes. NDSKR, vol 36, no. 3, 1999.

- Giurconiu M., Mirel I., Retezan A., Sarbu I. Hidraulica constructiilor si instalatiilor hidroedilitare. Editura Facla, Timisoara 1989.