|  | The 40th International Conference on Mechanics of Solids, Acoustics and Vibrations & The 6th International Conference on “Advanced Composite Materials Engineering” COMAT2016 & ICMSAV2016 Brasov, ROMANIA, 24-25 November 2016 |
| --- | --- |
|  | The 40th International Conference on Mechanics of Solids, Acoustics and Vibrations & The 6th International Conference on “Advanced Composite Materials Engineering” COMAT2016 & ICMSAV2016 Brasov, ROMANIA, 24-25 November 2016 |
|  | 6th International Conference Advanced Composite Materials Engineering  COMAT 2016 24-257 November 2016, Braşov, Romania |

ELASTICITY LAWS OF SOME UNIDIRECTIONAL FIBERS-REINFORCED LAMINAE SUBJECTED TO IN-PLANE LOADS

Ioan Szava1, Sorin Vlase2, Ildiko Renata Szava3, Florin Teodorescu-Draghicescu4

1 Transilvania University of Brasov, Brasov, ROMANIA,  e-mail: apukam27@gmail.com

2 Transilvania University of Brasov, Brasov, ROMANIA,  e-mail: svlase@unitbv.ro

3Transilvania University of Brasov, Brasov, ROMANIA,  e-mail: ildiko.munteanu@unitbv.ro

4 Politehnica University of Bucharest, Bucharest, ROMANIA,  e-mail: florin.teodorescu@ltpc.pub.ro

Abstract:  Distributions of the transformed compliances and rigidities in case of [45] unidirectional glass fibers-reinforced composite laminae versus the variation of their fibers disposal angle are computed and plotted. The basic elasticity constants of an epoxy/glass fibers unidirectional reinforced lamina with 40% fibers volume fraction, being in a stress plane state has been also determined. An [0] epoxy/boron fibers unidirectional reinforced lamina with 60% fibers volume fraction subjected to biaxial stresses σxx and σyy has been also considered in the computing model. Another lamina taken into consideration in this simulation process is a unidirectional [-45] epoxy/boron fibers-reinforced lamina with 60% fibers volume fraction subjected to biaxial stresses σxx and σyy to compute the lamina’s strains εxx, εyy and γxy. This computing model put into evidence the fact that although the loading of y-axis direction is half of that on x-axis direction, the εyy strain is eight times greater than that on x-axis direction which means that the tensile strength transverse to the fibers direction is very low in case of the [0] epoxy/boron lamina. Although the tangential stress τxy = 0, the biaxial stress field causes a γxy strain in case of a [-45] epoxy/boron lamina.

Keywords:  Transformed compliances, Transformed rigidities, Fibers-reinforced composites, Fibers volume fraction

1. INTRODUCTION

Fibers-reinforced polymer matrix composites belong to the class of heterogeneous and anisotropic materials, so their mechanics is much more complex than that of conventional materials. The basic element of a layered composite structure is represented by an individual layer called lamina reinforced with continuous unidirectional fibers inserted into a resin system called matrix. Basic assumptions in the description of the interaction between fibers and matrix in a lamina subjected to tensile loads, are [1], [2]:

- Both fibers and matrix behave as linear elastic materials;

- Initially, the lamina does not present residual stresses;

- The loads are applied parallel or perpendicular to the fibers direction;

- The matrix does not present voids and failures;

- The bond between fibers and matrix is perfect;

- The fibers are uniform distributed in matrix.

In a general case, the plane loading of a lamina is formed by three components that have been connected to the main directions in material [3], [4], [5-15]:

- The longitudinal loading, in which normal stress σ║ is parallel to fibers direction;

- The transverse loading, in which normal stress σ┴ acts perpendicular to fibers direction;

- The shear loading, determined by shear stresses τ# that act both parallel and perpendicular to fibers direction.

Three loadings can be defined on a representative volume element of the lamina. From a macroscopic point of view a lamina can be imagined as a continuous anisotropic homogeneous element in which the infinitely long fibers are inserted into the matrix. The lamina’s cross section is not homogeneous, so the computational approach is carried out with medium stresses. Normal stresses σ║ and σ┴ cause the strains ε║ and ε┴ on the respective loading directions. In the same time, normal stresses σ║ and σ┴ cause also a shrinkage on the lamina’s thickness direction, shrinkage that is often irrelevant in case of thin-walled structural elements [16-27].

2. COMPUTING EXAMPLES

2.1. Case of a [45] unidirectional glass fibers-reinforced lamina

A unidirectional [45] glass fibers-reinforced composite lamina being in a stress plane state is considered. The basic elasticity constants of this kind of lamina are: E║ = 47000 MPa; E┴ = 14800 MPa; υ┴║ = 0.3; G║┴ = 5700 MPa; and α = 0° – 90°. It is required to compute the transformed compliances and rigidities versus the variation of fibers’ disposal angle. Distributions of the transformed compliances are presented in Figs. 1–2. Distributions of the transformed rigidities r11, r22, r33, r12, r13 and r23 are presented in Figs. 3–4.

Figure 1:  Distributions of transformed compliances c11, c22 and c33

Figure 2:  Distributions of transformed compliances c12, c13 and c23

Figure 3:  Distributions of transformed rigidities r11, r22 and r33

Figure 4:  Distributions of transformed rigidities r12, r13 and r23 of [45] unidirectional glass fibers-reinforced lamina

2.2. Case of a 40% glass fibers volume fraction unidirectional reinforced lamina

An epoxy/glass fibers unidirectional reinforced lamina with 40% fibers volume fraction, being in a stress plane state has been considered. The input data regarding fibers and matrix properties are: EF = 73 GPa; EM = 3.6 GPa; υF = 0.25; υM = 0.35; the fibers volume fraction varies between 10% and 70%. The distributions of basic elasticity constants versus the fibers volume fraction for a unidirectional glass fibers-epoxy reinforced lamina are presented in Figs. 5–6.

Figure 5:  Basic elasticity constants E║, E┴ and G║┴ of an epoxy/glass fibers unidirectional reinforced lamina

Figure 6:  Poisson’s ratios ν┴║ and ν║┴ of an epoxy/glass fibers unidirectional reinforced lamina

2.3. Case of an [0] epoxy/boron unidirectional fibers reinforced lamina subjected to biaxial stresses

An [0] epoxy/boron fibers unidirectional reinforced lamina with 60% fibers volume fraction subjected to biaxial stresses σxx and σyy has been considered. The aim is to compute the lamina’s strains εxx and εyy. Following input data has been used: EF = 420 GPa; EM = 3.6 GPa; νF = 0.1; νM = 0.35; φ = 60%; α = 0˚; σxx = 1 GPa; σyy = 0.5 GPa. Stresses and strains are presented in Fig. 7.

σxx = 1 GPa

σyy = 0.5 GPa

x, ║

y, ┴

σxx

σyy

α = 0°

εxx = 0.0035

εyy = 0.029

φ = 60%

Figure 7:  Stresses and strains in an [0] epoxy/boron fibers unidirectional reinforced lamina

2.4. Case of an [-45] epoxy/boron unidirectional fibers reinforced lamina subjected to biaxial stresses

An [-45] epoxy/boron fibers unidirectional reinforced lamina with 60% fibers volume fraction subjected to biaxial stresses σxx and σyy has been considered. The task is to compute the lamina’s strains εxx, εyy and γxy. Following input data has been used: EF = 420 GPa; EM = 3.6 GPa; νF = 0.1; νM = 0.35; φ = 60%; α = -45˚; σxx = 1 GPa; σyy = 0.5 GPa. Fig. 8 presents the strains of an [-45] epoxy/boron fibers unidirectional reinforced lamina with 60% fibers volume fraction subjected to biaxial stresses σxx and σyy.

σxx = 1 GPa

σyy = 0.5 GPa

x

y

σxx

σyy

α = - 45°

εxx = 0.0442

εyy = 0.0028

φ = 60%

║

┴

Figure 8:  Stresses and strains in an [-45] epoxy/boron fibers unidirectional reinforced lamina

3. CONCLUSION

It is interesting to notice that although the loading of y-axis direction is half of that on x-axis direction, the εyy strain is eight times greater than that on x-axis direction which means that the lamina’s tensile strength transverse to the fibers direction is very low in case of an [0] epoxy/boron fibers unidirectional reinforced lamina (Fig. 7). Although the tangential stress τxy = 0, the biaxial stress field causes a γxy strain in case of an [-45] epoxy/boron unidirectional fibers reinforced lamina subjected to biaxial stresses (Fig. 8).

REFERENCES

- Cristescu ND, Craciun EM, Soos E., Mechanics of elastic composites, Chapman & Hall/CRC; 2003.

- Schürmann H., Konstruiren mit Faser-Kunststoff-Verbunden, Springer, 2005.

- Teodorescu-Draghicescu H, Vlase S., Homogenization and Averaging Methods to Predict Elastic Properties of Pre-Impregnated Composite Materials. Computational Materials Science, 50, 4, 2011, p. 1310–1314.

- Teodorescu-Draghicescu H, Vlase S, Scutaru ML, Serbina L, Calin MR., Hysteresis Effect in a Three-Phase Polymer Matrix Composite Subjected to Static Cyclic Loadings. Optoelectronics and Advanced Materials – Rapid Communications (OPTOELECTRON ADV MAT), Vol. 5, No. 3, 2011, p. 273-277.

- Teodorescu-Draghicescu H, Stanciu A, Vlase S, Scutaru ML, Calin MR, Serbina L., Finite Element Method Analysis Of Some Fibre-Reinforced Composite Laminates, Optoelectronics and Advanced Materials – Rapid Communications (OPTOELECTRON ADV MAT), Vol. 5, No. 7, 2011, p. 782-785.

- Stanciu A, Teodorescu-Draghicescu H, Vlase S, Scutaru ML, Calin MR., Mechanical Behavior of CSM450 and RT800 Laminates Subjected to Four-Point Bend Tests, Optoelectronics and Advanced Materials – Rapid Communications (OPTOELECTRON ADV MAT), Vol. 6, No. 3-4, 2012, p. 495-497.

- Modrea A, Vlase S, Teodorescu-Draghicescu H, Calin MR, Astalos C., Properties of advanced new materials used in automotive engineering. Optoelectronics and Advanced Materials – Rapid Communications (OAM-RC), Vol. 7, No. 5-6, 2013, p. 452–455.

- Heitz T, Teodorescu-Draghicescu H, Lache S, Chiru A, Calin MR., Advanced T700/XB3585 UD carbon fibers-reinforced composite, Journal of Optoelectronics and Advanced Materials (J OPTOELECTRON ADV M), Vol. 16, No. 5-6, 2014, p. 568-573.

- Teodorescu-Draghicescu H, Vlase S, Stanciu MD, Curtu I, Mihalcica M., Advanced Pultruded Glass Fibers-Reinforced Isophtalic Polyester Resin, Materiale Plastice (MATER PLAST), Vol. 52, No. 1, 2015, p. 62-64.

- Scutaru ML, Teodorescu-Draghicescu H, Vlase S, Marin M., Advanced HDPE with increased stiffness used for water supply networks, Journal of Optoelectronics and Advanced Materials (J OPTOELECTRON ADV M), Vol. 17, No. 3-4, 2015, p. 484-488.

- Niculita C, Vlase S, Bencze A, Mihalcica M, Calin MR, Serbina L., Optimum stacking in a multi-ply laminate used for the skin of adaptive wings. Optoelectronics and Advanced Materials – Rapid Communications (OAM-RC), 5, 11, 2011.

- Teodorescu-Draghicescu H, Scutaru ML, Rosu D, Calin MR, Grigore P., New Advanced Sandwich Composite with twill weave carbon and EPS. Journal of Optoelectronics and Advanced Materials (JOAM), Vol. 15, No.3-4, 2013, p.199–203.

- Teodorescu-Draghicescu H, Vlase S, Chiru A, Purcarea R, Munteanu V., Theoretical and Experimental Approaches Regarding the Stiffness Increase of Fibre-Reinforced Composite Structures. Proc. of the 1st Int. Conf. on Manufacturing Engineering, Quality and Production Systems (MEQAPS’09), Transilvania University of Brasov, Romania, WSEAS Press, 2009, p. 449–452.

- Vlase S, Teodorescu-Draghicescu H, Motoc DL, Scutaru ML, Serbina L, Calin MR., Behavior of Multiphase Fiber-Reinforced Polymers Under Short Time Cyclic Loading. Optoelectronics and Advanced Materials – Rapid Communications (OAM-RC), 5, 4, 2011.

- Vlase S, Purcarea R, Teodorescu-Draghicescu H, Calin MR, Szava I, Mihalcica M., Behavior of a new Heliopol/Stratimat300 composite laminate. Optoelectronics and Advanced Materials – Rapid Communications (OAM-RC), Vol.7, No.7-8, 2013, p. 569–572.

- Teodorescu-Draghicescu H, Vlase S, Goia I, Scutaru ML, Stanciu A, Vasii M., Tensile Behaviour of Composite Specimens Made From Chopped Strand Mat Reinforced Polyester Resin. 24th Danubia – Adria Symposium on Developments in Experimental Mechanics, 19-22 September, 2007, Sibiu, Editura Universităţii Lucian Blaga Sibiu, p. 255–256.

- Vlase S, Teodorescu-Draghicescu H, Calin MR, Serbina L., Simulation of the Elastic Properties of Some Fibre-Reinforced Composite Laminates Under Off-Axis Loading System. Optoelectronics and Advanced Materials – Rapid Communications, 5 (3–4), 2011, p. 424–429.

- Naughton BP, Panhuizen F, Vermeulen VC., The Elastic Properties of Chopped Strand Mat and Woven Roving in G.R. Laminae. Journal of Reinforced Plastics and Composites, 4 (2), 1985, p. 195–204.

- Teodorescu-Draghicescu H, Vlase S, Chiru A, Purcarea R, Munteanu V., Theoretical and Experimental Approaches Regarding the Stiffness Increase of Fibre-Reinforced Composite Structures. Proc. of the 1st Int. Conf. on Manufacturing Engineering, Quality and Production Systems (MEQAPS’09), Transilvania University of Brasov, Romania, WSEAS Press, 2009, p. 449–452.

- Purcarea R, Motoc DL, Scutaru ML., Mechanical behavior of a thin nonwoven polyester mat subjected to three-point bend tests, Optoelectronics and Advanced Materials – Rapid Communications, Vol. 6, No. 1-2, 2012, p. 214 – 217.

- Vlase S, Teodorescu-Draghicescu H, Calin MR, et al., Advanced Polylite composite laminate material behavior to tensile stress on weft direction. Journal of Optoelectronics and Advanced Materials (JOAM), Vol. 14, No. 7-8, 2012, p. 658–663.

- Modrea A, Vlase S, Calin MR, et al., The influence of dimensional and structural shifts of the elastic constant values in cylinder fiber composites. Journal of Optoelectronics and Advanced Materials (JOAM), Vol. 15, No. 3-4, 2013, p. 278–283.

- Niculita C, Gabor A, Gheorghe V, Calin MR, Scutaru ML., A new epoxy glass roving fabric material with a nonwoven PES fibers structure used in a composite laminates, Journal of Optoelectronics and Advanced Materials (JOAM), Vol. 15, No. 3-4, 2013, p. 176-181.

- Scutaru ML, Baritz M, Galfi BP., Radiation influence on micro-structural mechanics of an advanced hemp carbon hybrid composite, Optoelectronics and Advanced Materials – Rapid Communications (OAM-RC), Vol. 8, No. 11-12, 2014, p. 1145-1149.

- Scutaru ML., Toward the use of irradiation for the composite materials properties improvement, Journal of Optoelectronics and Advanced Materials (JOAM), Vol. 16, No. 9-10, 2014, p. 1165-1169.

- Scutaru ML, Baba M, Baritz MI., Irradiation influence on a new hybrid hemp bio-composite, Journal of Optoelectronics and Advanced Materials (JOAM), Vol. 16, No. 7-8, 2014, p. 887-891.

- Scutaru ML, Baba M., Investigation of the Mechanical Properties of Hybrid Carbon-Hemp Laminated Composites Used as Thermal Insulation for Different Industrial Applications, Advances in Mechanical Engineering, Article Number: 829426, 2014.