|  | The 2nd International Conference Computational Mechanics and Virtual Engineering COMEC 2007 11 – 13 OCTOBER 2007, Brasov, Romania |
| --- | --- |

MECHANICAL BEHAVIOUR OF NON-PRE-TENSIONED GLASS FABRIC REINFORCED COMPOSITE TUBES SUBJECTED TO INTERNAL PRESSURE

H. Teodorescu1, S. Vlase1, L. Scutaru1, R. Purcarea1

1 Transilvania University, Brasov, ROMANIA,  e-mail: draghicescu.teodorescu@unitbv.ro

Abstract: The paper presents a theoretical approach regarding the mechanical behaviour of non-pre-tensioned glass fabric reinforced composite tubes, subjected to internal pressure. The computing of stresses and strains is accomplished in the hypothesis of neglecting the temperature- and humidity variations on the composite material structure. The increase of loading capability of pre-tensioned tubes against the non-pre-tensioned ones is situated about 32%.

Keywords:  glass fabric, plain weave, pre-tensioning, loading capability, pre-tensioning pressure, PMC tubes

1. INTRODUCTION

The fabrics made from glass fibers are characterized by number of nodes on square centimeter, width, thickness, porosity (eye width), bending strength, surface appearance and applied treatments. The main weave modes are the plain weave (in which the warp- and weft threads pass recurrently one above the other), the twill weave (in which the fabric forms a characteristic model with diagonal lines at the fabric surface) and satin weave (in which the fabric surface is formed from threads belonging either to weft or to warp). The fibers weave mode, their thickness and twisting degree play a significant role on the mechanical features of the composite structure. Regarding the hollow composite structure, the best mechanical features can be obtained in case of structure’s reinforcement with thin fabrics, the weave mode being plain weave. The computing of stresses and strains is accomplished neglecting the temperature- and humidity variations on the composite material structure. It is assumed also that the tube plies are orthotropic and the entire tube wall thickness t is much smaller than its curvature radius r.

2. THEORETICAL APPROACH

A composite tube based on polyester resin reinforced with glass fibers (plain weave) is considered, tube made by winding of eight fabric plies and subjected at internal pressure (fig. 1). By t1 and t2 the warp respective the weft thickness threads are denoted, the thickness of both threads is considered equal and, by weave mode, they form together a fabric ply with the entire thickness t. A and C represent the axial respective the circumferential tube’s direction.

Therefore, the loadings of the tube wall are:

σC=p⋅rt,												(1)

σA=p⋅r2t,												(2)

τAC=0,												(3)

where A and C represent the axial/circumferential tube direction and p is the internal pressure. The composite tube’s strains and the one ply stresses are:

εA=1−υII⋅υII⊥EII⋅σC2K⋅t'+t'⋅EIIE−2υII,								(4)

εC=1−υII⋅υII⊥EII⋅σC2K⋅2t'+t'⋅EIIE−υII,								(5)

γAC=0,												(6)

σII 1=σC2K,								(7)

σII 2=σC2K,							(8)

σ 1=σC2K,								(9)

σ 2=σC2K,							             (10)

where:

K=t'2EIIE+EEII−2+1−υII⋅υII⊥;  t'=t1t=t2t,						             (11)

EII, E and υII represent the basic elasticity constants and σC is the medium stress that acts in the circumferential direction of the composite tube. At the Poisson ratio, the first index represents the shrinkage direction and the second one is the loading direction that produces this shrinkage.

C (y)

A (x)

┴1

║1

┴2

║2

t1

t2

r

t1 + t2 = t

Figure 1:  Schematic representation of glass fabric reinforced composite non-pre-tensioned tube

From the experimental results obtained on this kind of tube and from the micromechanical relations:

EII=ϕ⋅EF+EM1−ϕ,									             (12)

E=EM1+0,85⋅ϕ21−υM21−ϕ1,25+ϕ⋅EM1−υM2EF,							             (13)

G=GM1+0,6⋅ϕ0,51−ϕ1,25+ϕGMGF,									             (14)

υII=ϕ⋅υF+υM1−ϕ,									             (15)

υII⊥=υII⋅EEII,										             (16)

the following input data have been determined and presented in tables 1 – 3. The index F refers to the glass fiber and the index M to the matrix.

Table 1:  Basic elasticity constants for UP resin reinforced with glass fabric

|  | Units | Value |
| --- | --- | --- |
| Density | kg/m3 | 1750 |
| Young modulus, E║ | MPa | 28100 |
| Young modulus, E┴ | MPa | 8625 |
| Shear modulus, G# | MPa | 3105 |
| Fibers volume fraction, φ | % | 35 |
| Poisson ratio, υ┴║ | - | 0.36 |
| Poisson ratio, υ║┴ | - | 0.11 |
| Poisson ratio, υ┴┴ | - | 0.53 |

Table 2:  Basic elasticity constants for isotropic materials

|  | E-glass | UP resin |
| --- | --- | --- |
| Density [kg/m3] | 2500 | 1250 |
| Young modulus, E [MPa] | 73000 | 3900 |
| Shear modulus, G [MPa] | 29200 | 1375 |
| Poisson ratio, υ [-] | 0.25 | 0.42 |

Table 3:  Loading and geometric data

|  | Units | Value |
| --- | --- | --- |
| Tube’s diameter, D | mm | 80 |
| Number of fabric plies, n | - | 8 |
| Fabric plies thickness | mm | 0.437 |
| Tube wall thickness, t | mm | 3.5 |
| Internal pressure, p | MPa | 1.5 |
| Fabric winding angle, ω | ° | 0 |

The circumferencial stresses in tube’s plies loaded at internal pressure are:

σC i=p⋅rii=18tl i,											             (17)

where ri and tl I represent the plies radii respective the plies thicknesses given in table 4.

Table 4

| Plies | Plies radii | Plies thicknesses |
| --- | --- | --- |
| 1 | 0.218 | 0.437 |
| 1-2 | 0.437 | 0.875 |
| 1-3 | 0.656 | 1.312 |
| 1-4 | 0.875 | 1.75 |
| 1-5 | 1.093 | 2.187 |
| 1-6 | 1.312 | 2.625 |
| 1-7 | 1.531 | 3.062 |
| 1-8 | 1.75 | 3.5 |

According to relations (17) and with help of data presented in tables 1 – 3, the stresses and strains in tube’s plies can be computed. The results are presented in tables 5 and 6.

Table 5:  Composite non-pre-tensioned tube’s stresses and strains reinforced with glass fabric, loaded at 1.5 MPa internal pressure

|  | Ply 1 | Plies 1-2 | Plies 1-3 | Plies 1-4 |
| --- | --- | --- | --- | --- |
| εA [-] | 0.0024 | 0.0012 | 0.0008 | 0.0006 |
| εC [-] | 0.0067 | 0.0033 | 0.0022 | 0.0017 |
| γAC [-] | 0 |  |  |  |
| σC [MPa] | 137.89 | 69.32 | 46.46 | 35.03 |
| σII1 [MPa] | 93.86 | 47.18 | 31.62 | 23.84 |
| σII2 [MPa] | 206.87 | 103.99 | 69.7 | 52.56 |

|  | Ply 1 | Plies 1-2 | Plies 1-3 | Plies 1-4 |
| --- | --- | --- | --- | --- |
| σ1 [MPa] | 69.03 | 34.7 | 23.26 | 17.53 |
| σ2 [MPa] | 44.08 | 22.15 | 14.85 | 11.2 |
| τ 1,2 [MPa] | 0 |  |  |  |

Table 6:  Composite non-pre-tensioned tube’s stresses and strains reinforced with glass fabric, loaded at 1.5 MPa internal pressure

|  | Plies 1-5 | Plies 1-6 | Plies 1-7 | Plies 1-8 |
| --- | --- | --- | --- | --- |
| εA [-] | 0.0005 | 0.0004 | 0.0003 | 0.0003 |
| εC [-] | 0.0013 | 0.0011 | 0.0009 | 0.0008 |
| γAC [-] | 0 |  |  |  |
| σC [MPa] | 28.17 | 23.6 | 20.34 | 17.89 |
| σII1 [MPa] | 19.18 | 16.06 | 13.84 | 12.17 |
| σII2 [MPa] | 42.27 | 35.41 | 30.51 | 26.84 |
| σ1 [MPa] | 14.1 | 11.81 | 10.18 | 8.95 |
| σ2 [MPa] | 9 | 7.54 | 6.5 | 5.71 |
| τ 1,2 [MPa] | 0 |  |  |  |

3. CONCLUSIONS

The distributions of axial-, circumferential strains and stresses in tube’s plies are presented below.

| 1-2 1-8 1 | 1 1-2 1-8 |
| --- | --- |

REFERENCES

[1]	Schneider, W., Wärmeausdehnungskoeffizienten und Wärmespannungen von Glasfaser/Kunst-stoff-Verbunden aus unidirektionalen Schichten, Kunststoffe 61, No. 4, 1971, pp. 273-277.

[2]	Tsai, S.W., Hahn, H.T., Introduction to Composite Materials, Technomic Publishing Co., Westport, 1980.

[3]	Puck, A., Zum Deformationsverhalten und Bruchmechanismus von unidirektionalem und orthogonalem Glasfaser/Kunststoff, Kunststoffe 55, No. 12, 1965, pp. 913-922.

[4]	Puck, A., Das Knie im Spannungs-Dehnungs-Diagramm und Rissbildungs bei Glasfaser/ Kunststoffen, Kunststoffe 58, No. 12, 1968, pp.886-893.

[5]	Teodorescu, H., Rosu, D., Birtu, C., Teodorescu, F., The increase of cracking limits of glass-fabric/polyester-resin composite tubes, Magazine of Industrial Ecology, Bucharest, Nr. 10-12, 2000, pp. 20-23.

[6]	Goia, I., Teodorescu, H., Rosu, D., Birtu, C., The pre-tension of glass fiber-reinforced composite tubes. Experimental method, 17th Danubia-Adria Symposium on Experimental Methods in Solid Mechanics, Prague, 2000, pp. 111-112.