|  | 1st International Conference Computational Mechanics and Virtual Engineering  COMEC 2005 20 – 22 October 2005, Brasov, Romania |
| --- | --- |

MICROSTRUCTURAL CONSIDERATIONS

ON FATIGUE CRACKS

Prof. Cornel BIŢ, Eng., Ph.D.

TRANSILVANIA University, Braşov, ROMANIA

E-mail: cbit@unitbv.ro

Abstract: The paper is concentrated on some micro-structural issues concerning the intimate behaviour of materials subjected to fatigue cycles.

Keywords: fatigue, cracks, propagation laws

1. INTRODUCTION

The study of the fatigue cracks propagation laws occupies a very important place within the modern engineering design. The present-day fatigue research is concentrated on materials cracks behaviour, considering that such cracks are present to some degree in all mechanical structures. They may exist as basic defects in the constituent materials – assimilated to material deficiencies in the form of pre-existing flaws – or they may be induced in a certain engineering structure during the service life. The whole life time of a certain structure subjected to fatigue cycles (or to static loads as well) depends upon the way in which material cracks do propagate until the final failure.  On the other hand, from the methodological study point of view, there is a big difference in studying short fatigue cracks (taking into consideration different micro-structural issues) and long fatigue cracks, applying to a certain extension the laws of LEFM – Linear Elastic Fracture Mechanics.

2. MICROSTRUCTURAL CONSIDERATIONS ON FATIGUE CRACKS

The modern theoretical and experimental investigations on fatigue of metals are now largely concentrated on three important areas: fatigue crack nucleation, short crack growth and long crack propagation. It is known that, from the very beginning of the fatigue cycles, short cracks develop inside the material. Some of these short cracks continue to propagate during the fatigue cycles, changing into long cracks while others stop propagating especially due to their interaction with microstructural features. Initiation and growth of fatigue cracks were found to be strongly dependent both on microstructural features (second phase particles, grain boundaries etc.) and on their changes during the fatigue cycles [1]. This paper analyses some investigations carried out to study certain structural changes in an aluminium alloy subjected to fatigue cycles. The material used for the experimental investigations – aluminium alloy 6061 T651, with the chemical composition shown in table 1, was in form of rolled plates.

Table 1: Chemical composition of the aluminium alloy (wt%)

Element		Si	Fe	Cu	Mn	Mg	Cr	Zn	Ti	Al

Min.		0.40		0.15		0.8	0.04			balance

Max.		0.80	0.70	0.40	0.15	1.2	0.35	0.25	0.15

Fatigue specimens, in form of elliptical section, (fig.1a), were subjected to a constant axial load and to a constant amplitude sinusoidal bending moment until fractures occurred. All tests have been performed in a laboratory environment at room temperature. After failure, the specimens fatigue fractures surfaces have been studied using a scanning electron microscope and a metallographic microscope. Thus, some relevant micrographies were obtained. We have found a lot of physical parameters changed by fatigue: material resistivity and acoustic properties, changes of the mechanical, electrical and magnetic behaviour of the material. From all these changes this paper presents some important conclusions concerning a diffusion process of some manganese compounds under the action of fatigue cycles, (fig.1).

b. Metallographic micrography showing different manganese compounds developed within the immediate area of the fatigue crack  (x400)

a. Cross section of the specimens subjected to fatigue

c. Scanning electron micrography of fracture surface showing the manganese segregation (dark) separated due to a diffusion process (x3000)

d. Fracture surface detail. The direction of crack growth at the level of material grains is evident (x3000)

Figure 1: Fatigue fractures surfaces microstructural aspects showing a diffusion process induced by fatigue

The manganese compounds observed at the level of the investigated fatigue surfaces - could be the result of a diffusion process involving different one-dimensional faults (interstitial atoms, foreign atoms, second-phase particles etc.) with very important consequences for the fatigue crack propagation and short crack growth. Even if the material is not loaded, there does also exist a certain interaction between dislocations and one-dimensional faults. Cottrell and Bilby [4] have shown that, the number of foreign atoms migrating in a time t towards the length unit of a dislocation is given by:

n(t)=3⋅π213⋅A⋅D⋅tkT23⋅n0	                                					   (1)

where, D: the diffusion coefficient for foreign atoms, k: Boltzmann’s constant, T: temperature, t: time, n0: the number of foreign atoms per unit volume, A: an elastic interaction parameter. On the other hand it is known that the one-dimensional faults concentration is not uniform in a material, determining the development of a flux with particles, in accordance with Fick’s law [4]:

i= D·grad (N)                                                                                                                              (2)

where N represents the concentration of the foreign particles while i  is the number of foreign particles passing through the unit area in an unit time.

It is also to be mentioned that both the interaction between dislocations and foreign atoms and the migration of particles due to a gradient of concentration are strongly dependent on temperature. Returning to the starting problem the following model has been considered: under the action of the external forces, during the fatigue cycles, at a given moment a certain crystal is stressed in a certain way. At every fatigue cycles there exists a probability for this crystal to emit (because of stress), discreetly, a local quantity of energy at the level of dislocation, which may be written as:

Q=α⋅V⋅σM2+σm22⋅E                                                                                                                 (3)

where : a constant, V: the volume of the material per number of dislocations, m, M: the maximum and the minimum value of stress, E: material modulus in simple tension and compression.

This energy determines the increase of temperature at the level of the involved dislocation. In order to find out the variation of temperature in space and time we have to use the equation of heat propagation [1]:

divξ⋅gradT)=cv⋅ρm⋅∂T∂t,                                                                                                    (4)

where  is the thermic conductivity of the material, cv: the specific heat for constant volume, m: mass density.

For a homogeneous material, eq. (4) can be written as follows:

∂2T∂x2+∂2T∂y2+∂2T∂z2=1χ⋅∂T∂t,                                                                                                       (5)

where

χ=ξcvρm                                                                                                                            (6)

is the diffusivity.

A solution for eq. 5 is:

T=T0+ATK(x,y,z),                                                                                                               (7)

where T0 is the ambient temperature, AT: an amplitude constant while

K(x,y,z)=14⋅π⋅χ⋅tn2⋅e−r4χt

is Poisson’s nucleus for Cauchy’s problem in heat equation, having the following properties, [4]:

- Δ−∂χ∂t⋅Kr,t=0 for t> 0

- K(r,t)> 0  for t>0

- limt→0K(r,t)=0, the convergence being uniform

- Rnt→0K(r,t)dx=1 for t>0,

where r is the position vector and Rn is the n-dimensional space. In our case we have n=3 for point-dislocation, n=2 for linear dislocation and n=1 for bidimensional dislocation.

For n=3, using the property (d) it follows that:

Q=0QdQ=Vcv⋅ρmT−T0dxdydz=VcvρmATKx,y,z,tdxdydz=

=cvρmATVKx,y,z,tdxdydz=cvρmAT.                                                                                  (8)

It follows therefore:

AT=Qcvρm=α⋅Vcv⋅ρm⋅σM2+σm22E                                                                                                 (9)

The temperature at the level of a certain point (x,y,z) from the involved dislocation is:

Tx,y,z,t=T0+α0⋅V0cvρm⋅σM2+σm22E14πχt32⋅e−x2+y2+z24χt.                                                             (10)

In the same way, for n=2 and n=1 we have:

Tx,y,t=T0+α1⋅V1L⋅cv⋅ρm⋅σM2+σm22E14πχt32⋅e−x2+y24χt.                                                               (11)

(for a linear dislocation with dimension L)

and

Tx,t=T0+α2⋅V2S⋅cv⋅ρm⋅σM2+σm22E14πχt32⋅e−x24χt.                                                                     (12)

(for a bidimensional dislocation with area S).

The gradient of temperature created do play a very important part within the diffusion process observed on our specimens, (fig. 2).

T

# DIFFUSION

# DIFFUSION

T0

0                                                   x

Figure 2: The gradient of temperature determining the diffusion process

REFERENCES

[1] BIT, C., Contributions to the Fatigue Crack Propagation Laws for Aluminium Alloys,  Doctoral thesis, Transilvania University, Brasov, ROMANIA, 1996

[2] HUDSON, C. M., STEWARD, S. K., Compendium of Sources of Fracture Toughness and Fatigue Crack Growth Data for Metallic Alloys, Rangley Research Center, NASA

[3] TEODORESCU, V., Ecuatiile fizicii matematice, Universitatea Bucuresti, Bucuresti, 1980

[4] MOISIL, G.C., Termodinamica, Editura Academiei, Bucuresti, 1988.